Technical Data Sheet for Graphene For Li-PO Anode

Name:					Graphene for Anode

Form:						Powder

Colour:					Greyish Black

Particle distribution (D 50):		~18 m

Moisture:					0.5

Carbon content:				95%

Specific Surface area:			~500 g/cm2